## Slide 1
An overview on metals
0-Dimensional System: magic clusters
Growth of quantum-sized metallic films
One Dimensional System: Metal Atom Wires
Two Dimensional System: A brief overview of quantum growth
From precise structural control to property optimization
Nano Plasmonics
Chapter 4 Computational design of metal systems

## Slide 2: Outline of the Lecture
Fundamental of Plasmonics
Plasmonic Enhancement
Quantum Plasmonics: Landau Damping
Lycurgus cup, AD 400

## Slide 3
Why Plasmonics?
The long wavelength of light (≈ m) creates a problem for extending optoelectronics into the nanometer regime.
A possible way out of this dilemma is the conversion of light into plasmons.
They have much shorter wavelengths than light and are able to propagate electronic signals.
Notes: The spin flip rate is given by an Arrhenius law which describes thermally-activated hopping across an energy barrier E.
Contrary to other thermally-activated processes, such as diffusion, the attempt frequency is not related to vibrations, but to spin rotation (Larmor frequency in the internal magnetic field).

## Slide 4
What is a Plasmon ?
The electrons in a metal can wobble like a piece of jelly, pulled back by the attraction of the positive metal ions that they leave behind.
In contrast to the single electron wave function, a plasmon is a collective wave where billions of electrons oscillate in sync.
A plasmon is a density wave in an electron gas. It is analogous to a sound wave, which is a density wave in a gas consisting of molecules.
Plasmons exist mainly in metals, where electrons are weakly bound to the atoms and free to roam. The free electron gas model provides a good approximation.
Notes: The spin flip rate is given by an Arrhenius law which describes thermally-activated hopping across an energy barrier E.
Contrary to other thermally-activated processes, such as diffusion, the attempt frequency is not related to vibrations, but to spin rotation (Larmor frequency in the internal magnetic field).

## Slide 5: Plasmon: Collective Motion of Electrons
electron
ion
electric field:
restoring force:
oscillation frequency:
typical energy: 5~15eV

## Slide 6: Surface Plasmons in Thin Metal Films
Drude model
Condition
Energy
In thin film

## Slide 7: Surface Plasmon in Nanostructures
Classical picture
surface plasmon
energy in
spherical nanoparticles

## Slide 8
Surface Plasmon Polariton (SPP) and Localized Surface Plasmon (LSP)
SPPs occur at the interface between dielectric and metal, yielding evanescent fields in the two half spaces.

## Slide 9
Surface Plasmon Polariton (SPP) and Localized Surface Plasmon (LSP)
LSP

## Slide 10
1
2
3
4
5
The Plasmon Resonance
Right at the plasmon frequency p the electron gas has a resonance, it oscillates violently. This resonance frequency increases with the electron density n , since the electric restoring force is proportional to the displaced charge. Similar to an oscillating spring one obtains the proportionality: p  n
The plasmon resonance can be observed in electron energy loss spectroscopy (EELS). Electrons with an energy of 2 keV are reflected from an Al surface and lose energy by exciting 1, 2, 3,… plasmons. The larger peaks at multiples of 15.3 eV are from bulk plasmons, the smaller peaks at multiples of 10.3 eV from surface plasmons.
Notes: The spin flip rate is given by an Arrhenius law which describes thermally-activated hopping across an energy barrier E.
Contrary to other thermally-activated processes, such as diffusion, the attempt frequency is not related to vibrations, but to spin rotation (Larmor frequency in the internal magnetic field).

## Slide 11
How to Couple Light with Plasmons?
To combine optoelectronics with plasmonics one has to convert light into plasmons. This is not as simple as it sounds.
Bulk plasmons are longitudinal oscillations (parallel to the propagation direction), while photons are transverse (perpendicular to the propagation). They do not match.
Surface plasmons are transverse, but they are mismatched to photons in their momentum. The two E(k) curves never cross. It is possible to provide the necessary momentum by a grating, which transmits the wavevector k = 2/d (d = line spacing) (generally termed momentum compensation).
photonline
Notes: The spin flip rate is given by an Arrhenius law which describes thermally-activated hopping across an energy barrier E.
Contrary to other thermally-activated processes, such as diffusion, the attempt frequency is not related to vibrations, but to spin rotation (Larmor frequency in the internal magnetic field).

## Slide 12
Excitation of surface plasmon polaritons
Prism coupling
Grating coupling
Notes: The spin flip rate is given by an Arrhenius law which describes thermally-activated hopping across an energy barrier E.
Contrary to other thermally-activated processes, such as diffusion, the attempt frequency is not related to vibrations, but to spin rotation (Larmor frequency in the internal magnetic field).

## Slide 13
Excitation of surface plasmon polaritons
Excitation using highly focused optical beams
Near-field excitation
Principle of the detection of SPPs with a SNOM probe. (b) and (c) SNOM images, propagation of SPPs along gold nanowires (wavelength 633 nm).
Schematic of the excitation of a white-light continuum of SPPs and their observation through an index-matched oil-immersion lens.
Notes: The spin flip rate is given by an Arrhenius law which describes thermally-activated hopping across an energy barrier E.
Contrary to other thermally-activated processes, such as diffusion, the attempt frequency is not related to vibrations, but to spin rotation (Larmor frequency in the internal magnetic field).

## Slide 14
Low-Dimensional Plasmons in Nanostructures
Single electron waves become quantized by confinement in a nanostructure. Likewise, collective electron waves (i.e., plasmons) are affected by the boundary conditions in a thin film, a nano-rod, or a nano-particle.
Plasmons in metal nanoparticles are often called Mie-resonances (after Gustav Mie). Their resonance energy and color depend strongly on their size, similar to the color change induced in semiconductor nanoparticles by confinement of single electrons. In both cases, smaller particles have higher resonance energy.
Notes: The spin flip rate is given by an Arrhenius law which describes thermally-activated hopping across an energy barrier E.
Contrary to other thermally-activated processes, such as diffusion, the attempt frequency is not related to vibrations, but to spin rotation (Larmor frequency in the internal magnetic field).

## Slide 15
Fundamental of Plasmonics
Plasmonic Enhancement
Quantum Plasmonics: Landau Damping

## Slide 16: Contributed by
Prof. Zhenyu Zhang U of Tennessee => ICQD/USTC
Dr. Ke Zhao U of Tennessee => Rice U
Dr. Xiaoguang Li U of Tennessee => Fudan U/USTC
Dr. Youlin Song Zhengzhou U/U of Tennessee
=> Henan College of Education
Dr. Bo Persson Julich Center, Germany
Dr. Hongxing Xu IOP/CAS & Lund U
Dr. Baohua Gu ORNL
Dr. Nahla Hatab ORNL
Dr. Claudia Troparevsky ORNL/U of Tennessee
Dr. Di Xiao ORNL
Dr. Yu Jia Zhengzhou U/ORNL
Dr. Gyula Eres ORNL
Dr. Chun-Hway Hsueh UT=>Taiwan
Dr. Adolfo Eguiluz U of Tennessee

## Slide 17: Surface Enhanced Raman Scattering (SERS)
Challenges:
(a) still too weak to detect single molecules , making SERS an ensemble
average technique
(b) too few SERS-active “hot spots”
(c) lack of control: searching for “hot spots” by trial-and-error
Standing Puzzle: underlying mechanism for SERS still unclear
Fleischman, Hendra, McQuillan, (1974)
Jeamaire and Van Duyne,
(1977)
Enhancement factor:
105 - 106.

## Slide 18: Systems, Scales, Approaches, Main Findings
System:
Approach:
Science:
Quantum
many-body
theory
molecule
(2-3Å)
Molecule on
single substrate
New chemical
effect
S:1-10Å
Nanoparticle dimer
Around touching contact
ab initio
density functional
theory of real atom
Optimal gap size,
magentic moment
S:1-3nm
localized surface plasmon + photonic effect (SERS)
d~λ
b~λ
λ:102-103 nm
1D & 2D Nanoparticle
dimer arrays
Classical Electromagnetic
theory

## Slide 19: Prevailing Mechanism: Perpendicular Electric Field
electron energy
in molecule
electron energy
in metal
charge transfer
molecule vibration
photon energy
photon-electron coupling
Estimated chemical effect: MCH ~ 102
Selection Rule: Electric Field Parallel to Vibration
e-
Metal Substrate
Molecule
Q
B. N. J. Persson, Chem. Phys. Lett. 82, 561 (1981)

## Slide 20: New Enhancement Mechanism from Parallel Electric Field
e-
Metal
Substrate
R
bulk damping
surface damping
C = Vacuum Value (no molecule)
Nanoparticle
Estimated Chemical Enhancement MCH :
102 for nanoparticle,
6×103 for flat surface
Selection Rule: Electric Field Perpendicular to Vibration.
Molecule
(with molecule)
Q
B. N. J. Persson, K. Zhao, and Z. Y. Zhang, Phys. Rev. Lett. 96, 207401 (2006)

## Slide 21: Comparison of The Two Mechanisms for Chemical Enhancement
Model | Previous | New
Vibration Relative to Surface | Best perpendicular | Best perpendicular
Electric Field Relative to Surface | Perpendicular | Parallel
Electric Field Relative to Vibration | Parallel | Perpendicular
Enhancement | 102 on any kind of surface geometry | 102 on small nanoparticle, 6×103 on flat surface

## Slide 22: Systems, Scales, Approaches, Main Findings
System:
Approach:
Science:
molecule
(2-3Å)
S:1-10Å
S:1-3nm
d~λ
b~λ
λ:102-103 nm
Quantum
many-body
theory
Molecule on
single substrate
New chemical
effect
Nanoparticle dimer
Around touching contact
ab initio
density functional
theory of real atom
Optimal gap size,
magentic moment
localized surface plasmon + photonic effect (SERS)
1D & 2D Nanoparticle
dimer arrays
Classical Electromagnetic
theory

## Slide 23: Strong vs Weak Coupling of a Nanoparticle Dimer
Different physics expected for a dimer in different electronic coupling regimes.
Small gap (touching contact)
Strong Coupling
Large gap
Weak Coupling
electron cloud
Optical
Magnetic
All expected to be different in two regimes
Transport
Chemical
…
…
Notes: 23

## Slide 24: Silver Nanoparticle Dimers
S
[111]
d
(Ag14)2,t-t
S
[100]
d
(Ag14)2,p-p
d=2.2Å
d=2.0Å
t-t: tip-tip orientation p-p: plane-plane orientation
Real Atoms Study
(Ag18)2,t-t
S
[100]
d
(Ag18)2,t-t
S
[100]
d
d=1.9Å
d=1.9Å
K. Zhao, M. C. Troparevsky, D. Xiao, A. Eguiluz, ZZ, PRL 102, 186804 (2009)
Notes: 24

## Slide 25: Optimal Gap Size (Electrical Linear Response)
Existence of an optimal gap size in all types of dimers
Higher maximum polarizability in tip-tip orientation
S
S (unit: interlayer spacing d)
Pz: dipole moment
Optimal Gap Size
Jellium Model (Nordlander’s group: Nano Lett 09): Much larger nanoparticle dimers
Notes: 25

## Slide 26: “Bond” Breaking Picture for Optimal Gap Size
S (unit: interlayer spacing d)
Transfered Charge (e)
After “bond” breaks
(large S)
Polarizability decreases
with increasing S
Before “bond” breaks
(small S)
S
Polarizability increases
with increasing S
“bond”: a channel allowing charge
to flow between nanoparticles
Classical picture: monotoneously decreasing
Notes: 26

## Slide 27: Emergent Magnetic Moment
Even nonmagnetic nanoparticles may develop a net magnetic moment for S smaller than optimal gap size (OGS)
S
Magnetic Moment (μB)
S (unit: interlayer spacing d)
Optimal
Gap Size
Zero Field
Notes: 27

## Slide 28: Mechanism for Emergent Magnetism
S (unit: interlayer spacing d)
energy level (eV)
energy level (eV)
S (unit: interlayer spacing d)
S
energy level
e
e
e
e
LUMO
HOMO
zero magnetic
moment
nonzero
magnetic moment
spin down
spin up
Notes: 28

## Slide 29: Understanding Coupling from Orbital View
M. C. Troparevsky, K. Zhao, D. Xiao, A. Eguiluz, Z. Y. Zhang, Phys. Rev. B (2010)
HOMO

## Slide 30: Nonlinear Dielectric Response
S
Nonlinear starting from
a weak field
unit: d
M. C. Troparevsky, K. Zhao, D. Xiao, Z. Y. Zhang, A. Eguiluz, Nano Lett. 9, 4452 (2009)
(Å3)

## Slide 31: Increasing Dipole Moment in Nonlinear Regime
600
400
200
(Å3)
Nonlinear Regime
Charge Transfer Between NP

## Slide 32
Orbitals of Nonlinear Regime
The transition to the nonlinear regime is featured by the change of character of the HOMO.
P/E
(Å3)

## Slide 33: Microscopic Mechanism of Nonlinear Response
No field
Weak Field
Energy
High Field Energy
HOMO
LUMO
empty
empty
fractionally occupied
Breakdown of adiabaticity,
entering nonlinear regime
(Ag18)2,t-t
(Ag18)2,t-t

## Slide 34: Interplay Between Electric and Magnetic Degree of Freedom
Linear response
Nonlinear response
(Ag18)2,t-t
Nanoparticle Aggregates as Potential Multiferroic Materials

## Slide 35: Systems, Scales, Approaches, Main Findings
System:
Approach:
Science:
molecule
(2-3Å)
S:1-10Å
S:1-3nm
d~λ
b~λ
λ:102-103 nm
Quantum
many-body
theory
Molecule on
single substrate
New chemical
effect
Nanoparticle dimer
Around touching contact
Real atom ab initio
density functional
theory
Optimal gap size,
magentic moment
localized surface plasmon + photonic effect (SERS)
1D & 2D Nanoparticle
dimer arrays
Classical Electromagnetic
theory

## Slide 36: Collective Photonic Effect for SERS
=
×
By Mie theory
=
×
dipole moment

## Slide 37: Advantages of Nanoshell: Higher Enhancement
log10MEM
d
38nm
(35,38) nm
K. Zhao, H. X. Xu, B. H. Gu, and ZZ, J. Chem. Phys. 125, 081102 (2006)
silica core
silver shell
Nanoshell:
Halas & Co.

## Slide 38: Advantages of Nanoshell: Extra Tunability
log10MEM
d [nm]
701nm
785nm
950nm
r2 [nm]
r1=35 [nm]
Hot Volume (MEM>1010 )~ 1720 nm3
at Resonance
12
8
4
0
log10MEM
(r1,r2)
d

## Slide 39: Giant Electromagnetic Enhancement
log10MEM
λ [nm]
480 640 800 960 1120
d
2D dimer array
dimer
chain l
chain l+1
total dimer number: 400
total dimer
number in
each chain:
225
Additional enhancement on top of isolated dimer

## Slide 40: Finite Size Effect (Oscillatory Enhancement) in 1D Dimer Arrays
Type I oscillation ΔN refers to
enhancement with array length
Type II oscillation Δn refers to
enhancement along one fixed
array
ΔN 2×Δn
β
N/2
N
1
log10MEM
log10MEM
dimer index
n
1
N/2
N
N fixed
Y. L. Song, K. Zhao, and Z. Y. Zhang,
J. Chem. Phys. 129, 204506 (2008)

## Slide 41: Mechanism of Oscillatory Enhancement
The oscillation with total dimer number:
Approximation: All dipoles feel the same field
0
m
dipole index:
Similar mechanism responsible for the oscillation along a fixed array,
but oscillation period
d
dipole field from m to 0:

## Slide 42: Constant Enhancement in 2D Dimer Arrays
N/2
N
1
log10MEM
Enhancement essentially
a constant for large N

## Slide 43
Highest EM enhancement: 4.5×1013
Additional enhancements due to long-range photonic effects
Collective photonic coupling effect – Fantasy, or Reality???
Zhao, Xu, Gu, Zhang, 2006,
J. Chem. Phys. 125, 081102.
Notes: Closely packed nanostructure not necessarily the best

## Slide 44
Highest EM enhancement: 4.5×1013
Additional enhancements due to long-range photonic effects
Collectivephotonic coupling effect – Fantasy, or Reality???
Zhao, Xu, Gu, Zhang, 2006,
J. Chem. Phys. 125, 081102.
Experimental Proof using gold bowties
Notes: Closely packed nanostructure not necessarily the best

## Slide 45: EBL and Reactive Ion Etching (RIE)
Developer
Lift
Off
Remover
RIE
Au Deposition
Si wafer
Resist
EBL generates high resolution features with arbitrary patterns
Positive Resist- expose part is removed; negative resist-expose part remains
Deposition of a Cr adhesion layer (8 nm)
RIE used to generate deep trench structures on silicon substrate
Notes: Conventional techniques vs Improved EBL technique

## Slide 46
Fabrication of Elevated Gold Nano-Bowtie
Close the gap beyond the EBL limit
Tunable gap size, density, shape and morphologies
Fully decoupled from substrate
Serving as a plasmonic nanoantenna
7.5 nm

## Slide 47: Effect of Nanostructures – Size and shape
Bowtie gives the best performance
Notes: Similar to previous studies

## Slide 48: Effect of Si Post – FDTD Simulations
E field enhanced by using elevated bowties

## Slide 49: Systematic studies of Gap Size on SERS
1
µ
m
100 nm
1
µ
m
100 nm
100 nm

## Slide 50: Gap-dependent SERS enhancement
1
µ
m
100 nm
1
µ
m
100 nm
100 nm
Notes: Enhancement on a single bowtie

## Slide 51: Power Law Dependent SERS on Gap Size
When gap size is sufficiently small, E only weakly depends on gap size (d)
(b)
SERS enhancement
A, m=-2.29
B, m=-2.19
C, m=-2.26
|E|4 = Adm
E ~ d-0.55
m = -2.2

## Slide 52: Power Law Dependent SERS on Gap Size
Max |E|4 enhancement
FDTD Simulation closely
correlates
With
experimental
results
Tip sharpness
w affect on E
Notes: Not been reported previously

## Slide 53: Collective Photonic Effect
B, 785 nm
A, 2 mm
C, 300 nm
C ccd = rrd = 300 nm
2 mm
2 mm
A ccd = rrd = 2 mm
B ccd = 785 nm, rrd = 2 mm
(a)

## Slide 54: Concurrent Multiscale Approach
Classical EM
for separated nanoparticles
DFT for touching
contact or molecular junction, but only small systems
Concurrent Multiscale
DFT
Classical
Charge
Matching

## Slide 55: Quantum Plasmonics
Xiaoguang Li (李晓光)
Di Xiao（肖笛）
Jian Shen（沈健）
Hanno Weitering
Zhenyu Zhang（张振宇）
Fudan University
University of Tennessee, Knoxville
University of Sci. & Tech. of China
03/05/2012

## Slide 56: Go Beyond The Classical Study
Quantum picture
A quasiparticle of the excited system
Classical picture
Charge density wave
Charge
Density
Collective Motion of Electrons

## Slide 57: Energy Tunability of Plasmon in Nanostructures
E. Prodan and P. Nordlander and N. J. Halas,
Nano Letters, 3, 1411--1415, (2003)
E. Prodan and C. Radloff and N. J. Halas and P. Nordlander,
Science, 302, 419-422, (2003)
Hybridization model

## Slide 58: Spectra of Single Electron-Hole Pairs and Collective Plasmon Mode
Landau Damping
Transition from plasmon to single electron-hole pair
Upper boundary
Lower boundary
plasmon
electron-hole
pairs
longitudinal wave
can not couple with light
q
Upper boundary
Lower boundary
q
Small q
Large q
Bulk Plasmon

## Slide 59: Linewidth of Plasmon in Nanostructures
  Plasmon to photon
    radiation damping (solved with classical theory)
  Plasmon to electron-hole pairs
    intrinsic Landau damping (quantum is needed)
Drude model
intrinsic damping
input parameter
Size dependence of intrinsic damping with quantum study
We expect high
Quality Factor:
intrinsic width
bulk property
confinement
R
A. Kawabata and R. Kubo, JPSJ, 21, 1765-1772, (1966)
U. Kreibig and C. v. Fragstein, Z. Physik, 224, 307--323, (1969)
dielectric function:
spherical particle

## Slide 60: Surface scattering and Landau damping
Classical picture
electron-hole
pairs
Quantum picture
A. Kawabata and R. Kubo, Journal of the Physical Society of Japan, 21, 1765-1772, (1966)

## Slide 61: Methods
Homemade code
  Ag (Wigner-Seitz radius rs=3.0 a.u.)
  the monolayer thickness 0.236 nm in Ag(111) direction as the unit of length
Ground state
  Local Density Approximation
  Jellium background
Excited state
  Random Phase Approximation
    real-space basis set
      scan energy for absorption peaks, limited by energy broadening
    electron-hole pair basis set
      solve the energy of plasmon modes directly

## Slide 62: Thickness Dependence of Plasmon in Thin Films
Energy (eV)
Linewidth (eV)
thickness increasing
interacting
initial broadening
Absorption
Energy (eV)
thin film
Thickness (monolayer)
Oscillatory Linewidth

## Slide 63: Comparison of Two Basis Sets
Real-space basis
Electron-hole basis
density-density response function
state-state response function
interaction
absorption
Energy eigenstates and corresponding absorption
Energy (eV)
Energy (eV)
energy broadening
interaction
absorption
absorption

## Slide 64: Band Structures and Electron-Hole Absorption Spectra in Thin Films
electronic subbands:
electron-hole
pairs:
Intra-subband:
Lower energy, carry most of spectral weight, important for the energy of plasmon
Inter-subband:
Important for the linewidth of plasmon
confined
extended
Absorption spectrum

## Slide 65: Landau Damping of Plasmon and Electron-Hole Pair Spectra
Absorption spectrum
Near degenerate
multiple plasmon modes

## Slide 66: Prototype Quantum Systems
nanoshell
0D
coaxial nanotube
1D
thin film
2D
symmetric antisymmetric
symmetric antisymmetric
0D & 1D
2D
L=1
(dipole approximation)
L=1; k
k
momentum dependence
d
d
d
size dependence
R
R
Plasmon
building block

## Slide 67: Energy and Landau Damping of Plasmon
nanoshells
coaxial nanotubes
thin films

## Slide 68
  In metal nanostructures, the oscillation of Landau damping, lacking within a classical surface scattering picture, offers unique opportunity to suppress it for longer plasmon lifetime.
This oscillatory effect is due to the discretization of electron-hole pair energy by quantum size effect, and the additional near degenerate multiple plasmon modes.

## Slide 69: A More Realistic System: Thin Film on Substrate
Si
Mg
Air
Absorption includes three parts:
1. Free electrons in Metal (quantum)
2. Screening charges in substrate (classical)
3. Interface charges (classical)
Magnesium
Silicon
Computational Method:
1. LDA for ground states with jellium approximation
2. Linear response theory for excited states
Silicon Surface
Magnesium Surface
Notes: structure
experimental observation
theoretical setup (we want to know which part of the absorption is from the thin film itself)

## Slide 70: Experimental Results for Plasmon in Thin Films
What is the difference from the semi-infinite system?
multipole plasmon
with different dispersion
Multipole
plasmon
the position of the surface peak
Surface
plasmon
the additional
extra peak
Extra
Peak
Bulk
plasmon
Absorption (arb.u.)
Energy (eV)
Energy (eV)
Absorption (arb.u.)

## Slide 71: Previous Theoretical Results for Free-standing Thin Film: Thickness Dependence of Plasmon in Thin Films
Energy (eV)
Linewidth (eV)
270
thickness increasing
interacting
initial broadening
Absorption
Energy (eV)
thin film
Thickness (monolayer)
oscillation!

## Slide 72: Theoretical Results
Energy (eV)
Absorption (arb.u.)
Mg electrons
Substrate
Total
plasmon enhanced substrate absorption
Si surface plasmon
Free-standing
Mg thin film
Mg thin film
on Si substrate

## Slide 73: Theoretical Results and Hybridization Model
Energy (eV)
Sym
Asym
Strong
Interaction
Weak
Interaction
Asym
Sym
Free standing
Mg film
Mg film
on Si substrate
Energy (eV)
Momentum ( )
Momentum ( )
Asym
Sym
Asym
Sym

## Slide 74: The Extra Peaks
Work function 3.66 eV
Absorption (arb.u.)
Energy (eV)
Rs = 2.66
Rs = 3.00
Rs = 3.66
Momentum ( )
Energy (eV)
The extra peak is due to
single electron-hole excitation
Extra Peak

## Slide 75: Another Mode: Multipole Plasmon
K.-D. Tsuei and E. W. Plummer and A. Liebsch and K. Kempa and P. Bakshi,
Phys. Rev. Lett., 64, 44--47, (1990)
What will happen as the confinement is applied?
Surface Plasmon
Multipole
Surface Plasmon
Semi-infinite film
Notes: another interesting collective mode
different density oscillation
different dispersion

## Slide 76: Negative Dispersion of Multipole Plasmon
Negative Dispersion
Bulk Plasmon
Multipole
Surface Plasmon
Surface
Plasmon
Extra
Peaks
Semi-infinite film
multiple plasmon
Surface plasmon

## Slide 77: Spectra of Thin Films with Different Thickness
D=2
D=3
D=4
D=5
Momentum ( )
Energy (eV)
Momentum ( )
Momentum ( )
Momentum ( )

## Slide 78: Difference between EELS and Simulation
In EELS (Electron Energy Loss Spectroscopy):
Momentum ( )
Energy (eV)
EELS measures the absorption for a certain angle but not a certain momentum.
Line for the measurement at different angles
12
18
6

## Slide 79: Summary
The similarity between the plasmon modes in thin films and semi-infinite films can be explained by the hybridization model.
The extra peak observed in the thin film is due to the single electron-hole excitation.
In contrast with the semi-infinite films, the multipole plasmon shows negative dispersion in thin films.